| WOOD veneered paneling product specification in CSi 3-part format | Decospan Belgium Lageweg 33 8930 Menen België (Belgium) United States Mr. Jeramy Nichols Crown Marketing P 1289 N. Fordham Blvd, Suite A-355 Chapel Hill, NC 27514 Phone: (919) 442-1091 Fax: 800-810-3081 Website: www.shinnoki.com E-mail: info@shinnoki.com |
| --- | --- |

GENERAL NOTES TO SPECIFIER: THE FOLLOWING PRODUCT SPECIFICATION LANGUAGE HAS BEEN PREPARED TO ASSIST DESIGN PROFESSIONALS IN SPECIFYING “SHINNOKI” wood VENEERED PANELing IN EXISTING 3-PART SPECIFICATIONS FOR CASEWORK, furniture, wall PANELING, ceiling paneling, and decorative wainscoting. SAMPLE LANGUAGE IS PROVIDED FOR APPLICABLE ARTICLES IN PART 1–GENERAL AND PART 2–PRODUCTS FOLLOWING THE CONSTRUCTION SPECIFICATION INSTITUTE’S SECTIONFORMAT. BECAUSE OF THE VARIATION IN SPECIFICATION SYSTEMS CURRENTLY IN USE, ARTICLE AND PARAGRAPH NUMBERS AND TITLES MAY DIFFER SOMEWHAT THAN PRESENTED HEREIN. THE SAMPLE LANGUAGE SHOULD BE EDITED ACCORDINGLY TO FIT EACH FIRM’S SPECIFICATIONS. THIS SECTION ASSUMES THE PROJECT MANUAL CONTAINs COMPLETE DIVISION 01 DOCUMENTS, INCLUDING the following SECTIONS: 012513 PRODUCT SUBSTITUTION PROCEDURES 013300 SUBMITTAL PROCEDURES 016200 PRODUCT OPTIONS 016600 PRODUCT STORAGE AND HANDLING REQUIREMENTS 017400 CLEANING AND WASTE MANAGEMENT 017700 CLOSEOUT PROCEDURES, AND 017800 CLOSEOUT SUBMITTALS. CLOSE COORDINATION WITH DIVISION 01 SECTIONS IS REQUIRED. IF THE PROJECT MANUAL DOES NOT CONTAIN THESE SECTIONS, ADDITIONAL INFORMATION SHOULD BE INCLUDED UNDER THE APPROPRIATE ARTICLES. NOTES TO THE SPECIFIER ARE CONTAINED IN BOXES AND SHOULD BE DELETED FROM FINAL COPY. GREEN TEXT AND NOTES RELATE TO LEED® PROJECTS AND CAN BE DELETED IF THE PROJECT IS NOT INTENDED TO ATTAIN LEED® CERTIFICATION. OPTIONAL ITEMS REQUIRING SELECTION BY THE SPECIFIER ARE ENCLOSED WITHIN BRACKETS, E.G. [35] [40] [45]. MAKE APPROPRIATE SELECTIONS AND DELETE OTHERS. ELECTRONIC VERSIONS OF THIS SPECIFICATION UTILIZE AUTOMATIC PARAGRAPH NUMBERING. WHEN EDITING IS COMPLETE, DELETE ALL TEXT ON THIS PAGE, THEN REMOVE THE SECTION BREAK AT THE TOP OF THE NEXT PAGE TO REMOVE THIS INTRODUCTORY SECTION FROM THE DOCUMENT.

SPECIFICATION BEGINS ON THE FOLLOWING PAGE.

# General

## Summary

SHINNOKI VENEERED PANELing CAN BE USED IN A VARIETY OF interior APPLICATIONS.  SOME OF THE MORE COMMON USES ARE INDICATED BELOW.  DELETE OR ADD FROM THE LISTED ITEMS AS APPLICABLE.

### Section Includes:

#### Wood Veneered Paneling used in:  [Casework,] [furniture,] [decorative wainscoting,] [wall paneling,] [ceiling paneling,] [other].

### Related Sections:

#### Division 01: Administrative, procedural, and temporary work requirements.

## References

### Reference Standards:  Current edition at date of bid.

#### U.S. Green Building Council (USGBC):  Leadership in Energy and Environmental Design (LEED®) Green Building Rating System™.

## Submittals

### Reference Section “013300  Submittal Procedures.”

### Product Data: For each type of product[, including finishing materials and processes].

### Samples for Verification:  2.5 by 6.5 inches, for each color as specified.

### LEED® Submittals:

include if paneling used is one of NINE (9) veneers availabe in fsc-certified wood:  [Ivory Aspen] [Bright Maple] [Milk Oak] [Desert Oak] [Mystery Oak] [Granite Walnut] [Smoked Walnut] [Espresso Beech] [Chocolate Oak]

#### Credit MR 7 – FSC Certified Wood:  Chain-of-custody certificates for products containing certified wood.

#### Credit IEQ 4.4 - Low-Emitting Materials—Composite Wood & Agrifiber Products:  Product data for products containing composite wood or agrifiber products or wood glues indicating that they do not contain urea-formaldehyde resin.

## Quality Assurance

### Qualifications:

#### Manufacturer:

##### Single firm providing both panel and veneer of finished product.

##### Minimum five years experience in producing veneered paneling.

#### Fabricator Qualifications:  Shop that employs skilled workers who custom-fabricate products similar to those required for this Project and whose products have a record of successful in-service performance

#### Quality Standard:  Unless otherwise indicated, comply with [AWS's "Architectural Woodwork Standards."].

##### Provide AWS Quality Certification Program [labels] [and] [certificates] for woodwork[, including installation].

#### Forest Certification:  Provide paneling produced from wood obtained from forests certified by an FSC-accredited certification body to comply with FSC STD-01-001, "FSC Principles and Criteria for Forest Stewardship."

## Delivery, Storage, and Handling

### Reference Section “01 66 00  Product Storage and Handling Requirements.”

### Packaging:

decospan paneling is provided with a 0.5 mm uv-inhibiting peel coat on the veneered side.

#### Package panels with a UV-inhibiting, protective peel coat, to be removed only after installation.

#### Include the following information:

##### Thickness and color.

##### Manufacturer's contact information.

### Environmental Limitations:  Do not deliver or install paneling until building is enclosed, wet work is complete, and HVAC system is operating and will maintain temperature and relative humidity at occupancy levels during the remainder of the construction period.

### Delivery of panels in original packaging not less than 10 days prior to start of installation.

### Store materials minimum 6 inches above ground on framework or blocking, providing for adequate air circulation.

### Protect edges and corners of sheet materials from damage.

# Products

## Manufacturer

### Decospan, www.shinnoki.com, (919) 442-1091.

## Wood Veneered Paneling

### Panel Characterstics:

veneer UTILIZES a mix-match jointing pattern of selected grain characteristics, comprised of 20 flitches.  there are sixteen (16) different veneers, available in the following colors :

#### Veneer Species:  [Ivory Aspen] [Bright Maple] [Sand Ash] [Milk Oak] [Desert Oak] [Mystery Oak] [Dusk Fraké] [Granite Walnut] [Smoked Walnut] [Tempered Fraké] [Bronze Curupixa] [Shadow Macassar] [Espresso Beech] [Midnight Ash] [Chocolate Oak] [Nero Lati].

##### Sides:  [Single] [Double].

##### Gloss:  10.

all colors are finished as brushed, except for the following colors, which are sealed:
	Bright Maple
	Shadow Macassar
	Espresso Beech

##### Finish:  [Brushed] [Sealed]

for single-sided panels, backing melamine is a light-colored melamine.  dark color option is available for the following species/colors:  [DUSK FRAKÉ], [SHADOW MACASSAR], [ESPRESSO BEECH], [MIDNIGHT ASH], [CHOCOLATE OAK], AND [NERO LATI].

##### Backing:  [Light, NCS 1005-Y50R] [Dark, NCS S7500-N]-colored melamine.

finish is an 8-layer, polyurethane, stain-lacquer, protected by a peel coat.  DECOSPAN DOES NOT ADVISE THE USE OF THESE VENEERED PANELS IN ANY EXTERIOR APPLICATION.

#### Finish:  Acrylic-Polyurethane.

#### Core:  Medium-Density Fiberboard:  ANSI A208.2, Grade MD[, made with binder containing no urea formaldehyde].

#### Board Size:  [108.5 x 48.5 inches; 9 feet 0.5 inches x 4 feet 0.5 inches] [Custom].

#### Board Thickness:  [19 mm] [Custom].

#### Plies:  3-ply.

PANEL EDGES ARE SQUARE.  HOWEVER, a small curved edge is possible with the addition of edgebanding, which  has A micro-beveled EDGE

#### Edge Configuration: Square.

### Properties:

paragraphs 1 – 9 are european test results.

#### Indentation; EN 1534:  >/= 20 Newton/mm2.

#### Abrasion; EN 14354/EN112,73.XX:  3,000 Revolutions.

#### Lacquer Adhesion; EN ISO 2409:  Class 2.

#### Chemical Agent Resistance; EN 423/Part 2:  Grade 4.

#### Lacquer Hardness; DIN 53154:  2 Newton.

#### VOC Loss; EN 664:  <2.1%.

#### Formaldehyde emission; E1 (EN 717-1):  Class (ppm) E1 (non added formaldehyde).

#### Formaldehyde emission; E1 (EN717-2):  Class (mg/m³h) E1 (non added formaldehyde).

#### Fire reaction and smoke generation; EN 13823:  Class C1 Bfl s1.

#### Rapidly renewable product manufactured using low-emitting, urea formaldehyde-free binders; ASTM E 1333.

##### 1/4" inch thick [1-ply] [3-ply] vertical grain:  0.07 ppm.

##### 1/2" inch thick [1-ply] [3-ply] vertical grain:  0.02 ppm.

##### 1/3" inch thick 3-ply cross laminated core:  0.10 ppm

##### 1/3" inch thick 1-ply vertical grain:  0.10 ppm.

NINE (9) veneers are availabe in fsc-certified wood:  [Ivory Aspen] [Bright Maple] [Milk Oak] [Desert Oak] [Mystery Oak] [Granite Walnut] [Smoked Walnut] [Espresso Beech] [Chocolate Oak]

#### Certified to FSC STD-04-004.

## accessories

### Pre-finished Edge Banding

standard edgebanding is 0.6 mm matching veneer.  ABS  is available with matching colors (1 mm ABS GLUED TO 0.5 MM VENEER).

#### Material:  [Matching veneer] [ABS, with a no-shelf life adhesive].

keep the following paragraph if veneered abs edge banding is used.

#### Thickness:  1.5 mm.

#### Width[s]:  [24] [ 44] mm.

### Touch-Up Marker Pens and Spray Cans

# Execution

## 3.1	INSTALLATION

### Protect exposed finishes and surfaces from construction damage.  Remove peel coat only after installation.

End of Section

This specification was prepared specifically for Decospan. Comments or suggestions for improvement should be addressed to (206) 412-9705 or Crown Marketing, P 1289 N. Fordham Blvd, Suite A-355, Chapel Hill, NC 27514, (919) 442-1091.

Issue Date: May 2010.